## Slide 1: Magnet options and timeline P. Ferracin Lawrence Berkeley National Laboratory
Snowmass at LBNL
LBNL
December 10, 2021

## Slide 2: Outline
Superconducting materials
Field levels
  5-9 T 11-13 T 14-16 T Beyond 16 T
Some considerations on timelines

## Slide 3: Superconducting materials
Nb-Ti
5 - 9 T
The “workhorse”
Small filaments
Ductile and cheap
Nb3Sn
11 – 16 T
Strain sensitive and brittle
Reaction to 670 C
Larger filaments
Bi2212
Round strand -> Rutherford cable
Reaction to 900 C and 50 bar in O2
Strain sensitive
Beyond 16 T
REBCO
Tape
No reaction
Strain sensitive
Angle dependence of Je

## Slide 4: Superconducting materials
Typical Je in accelerator magnets
Je = Strand current / strand area
Typically magnets operate at 80% of the limits
So,
  Nb-Ti up to 10 T
  Nb3Sn up to 16 T

## Slide 5: Outline
Superconducting materials
Field levels
  5-9 T 11-13 T 14-16 T Beyond 16 T
Some considerations on timelines

## Slide 6: Overview of Nb-Ti and Nb3Sn dipole magnets
By L. Bottura

## Slide 7: The 5-9 T field level (Nb-Ti)
By L. Bottura

## Slide 8: The 5-9 T field level (Nb-Ti)
Accelerator magnets fabricated in large series and installed in particle colliders (except SSC)
From 4.4 T in Tevatron to 8.3 T (9 T ultimate) in LHC
Tevatron
HERA
RHIC
SSC
LHC
Not in scale

## Slide 9: The 5-9 T field level (Nb-Ti)
Nb-Ti magnets for the HL-LHC currently under fabrication: up to 6.6 T

## Slide 10: The 11-13 T field level (Nb3Sn)
By L. Bottura

## Slide 11: The 11-13 T field level (Nb3Sn)
IR quadrupole for HL-LHC: MQXF
Arc dipole for HL-LHC: 11T
Accelerator quality magnets
Short model and prototype program completed, series started

## Slide 12: The 14-16 T field level (Nb3Sn)
By L. Bottura

## Slide 13: The 14-16 T field level (Nb3Sn)
FNAL MDPCT: 14.5 T
CERN FRESCA2: 14.6 T
Short models, with aperture, but not yet accelerator quality

## Slide 14: The 14-16 T field level (Nb3Sn)
By L. Bottura

## Slide 15
LBNL HD1, CERN RMM and ERMC: all reached (and passed) 16 T
Limit of Nb3Sn reached so far only in short models with simple coil geometries (no bore, racetrack…)

## Slide 16: Beyond 16 T 20 T hybrid zoo
Preliminary design studies
  Different HTS and Nb3Sn coil lay-outs for 20 T hybrid magnets

## Slide 17: Beyond 16 T MDP current activities
HTS insert coil (2-5 T) being fabricated at
  BNL
    Racetrack REBCO CORC coils inside common coil
  FNAL
    SMCT inserts in CT and SMCT outserts
  LBNL
    CCT inserts in CCT outserts
Similar activities carried out in Europe

## Slide 18: Outline
Superconducting materials
Field levels
  5-9 T 11-13 T 14-16 T Beyond 16 T
Some considerations on timelines

## Slide 19: Some considerations on timelines
Project timeline
  10+ years, considering short models, prototype, and series
    Time can change significantly depending on the size of the project (HL-LHC: 1.5 km; FCC: 100 km)
R&D timeline
  Time towards a project
For the Nb-Ti 5-9 T level and the Nb3Sn 11-13 T level
  Accelerator quality magnets fabricated or being fabricated in series production
    No need of “major” R&D (and a little bit of optimism….)
For the Nb3Sn 14-16 T level
  We need to fill the gap between R&D (“short”) magnets to accelerator quality (“reasonably long”) magnets
  Possible goal for the next ~10+ years: long accelerator quality Nb3Sn magnet (a prototype) in the 14-16 T field level
For the ~20 T level
  We are still working on small HTS insert coils, without significant experience in hybrid magnets
  Major R&D effort to be carried out (currently one of the key area of the US MDP program)
  Possible goal for the next ~10+ years: short model with sizable aperture