## Slide 1
A collaboration framework to advance high temperature superconducting magnets for accelerator facilities
Tengming Shen (US PI), Lawrence Berkeley National Laboratory
Mukesh Dhakarwal (KEK) for Toru Ogitsu (Japan PI), KEK
With Xiaorong Wang (US CO-PI), Lawrence Berkeley National Laboratory, Ramesh Gupta, (US CO-PI), Brookhaven National Laboratory, and Naoyuki Amemiya (Japan CO-PI, Kyoto University).
The 45th meeting of the US-Japan Joint Committee on High Energy Physics,
May 22-23, 2023, University of Hawaii

## Slide 2: Who we are?
Kyoto Uni: Naoyuki Amemiya, Yusuke Sogabe, Guangwei Xu, Mao Shigemasa
KEK: Toru Ogitsu, Tatsushi Nakamoto, Michinaka Sugano, Masami Iio, Kento Suzuki, Mukesh Dhakarwal
BNL: Ramesh Gupta, Piyush Joshi, Mithlesh Kumar
LBNL: Chris Reis, Laura Garcia Fajardo, Tengming Shen, Xiaorong Wang
Members of the US Magnet Development Program
Peter Hosemann
Graduate students
Early Career Scientists

## Slide 3: Why study HTS magnets?
High field frontier – enable frontier accelerator, fusion, and scientific facilities.
High temperature frontier – reduce the reliance on liquid He supply
(courtesy of D. Larbalestier, NHMFL)
Instruments 2020, 4(4), 30;
https://doi.org/10.3390/instruments4040030

## Slide 4: Our tasks
Task 1: HTS magnet technologies for high-radiation environment
  KEK, LBNL - Ceramic insulation, gamma-ray radiated epoxy resin composites, and neutron irradiation of REBCO tapes
Task 2: Stability, quench protection, and magnet safety
  Kyoto Uni., LBNL, BNL – quench modeling, experiments with single tapes and REBCO wires/cables.
Task 3: Measuring and modeling AC loss and field quality of HTS accelerator magnets
  Kyoto Uni., LBNL, KEK, BNL – magnets from C0 to C2, from modeling to experiments
Task 4: HTS/LTS high field hybrid accelerator dipole technology
  KEK – racetrack coils fab; BNL – test of KEK racetrack coils in 10 T background fields.
The current funding: 07/01/2021 - 06/30/2024; Will submit a renewal proposal in Dec 2023.

## Slide 5: Exchanges
Lecture (T. Shen) to Kyoto Uni. Students, April 21, 2023
Prof. Amemiya, Sept 2022, learned how to fabricate a terminal/joint with LBNL’s flute design with Hugh Higley, applied to his SCSC cable design,
And provided improvement.
Ogitsu and Shen in front of BELLE-II
April 16, 2023

## Slide 6: Task 1. Gamma ray radiation of epoxy resin composites and test
Epoxy resins are widely used in superconducting magnets.
By Chris Reis, LBNL, UCB, published with IEEE Trans. Appl. Supercond.
10.1109/TASC.2019.2898124
Selected for high-Lumi LHC
and AUP Nb3Sn Quads

## Slide 7: Task 2. Neutron irradiation of REBCO tapes made possible by unique facilities @ BR2 and Tohoku Uni.
Masami IIO, KEK
Helium ion implantation at LBNL/UC Berkeley
Sample prep + FIB-SEM @ UCB
HR-TEM of REBCO
at NCEM, LBNL

## Slide 8: Task 2. Improving quench detection for HTS magnets
Known and existing: cRIO + FPGA/PXI, LBNL MTF
developed for LTS magnets
Used to protect all MDP-LBNL Bi-2212 magnets.
RMS noises in 10-2 V.
Quench detection at 50 – 100 mV.
Extraction at
t = 0 s.
MIITS/time budget:
Detection
Protection
MIITS/time budget:
Detection
Protection
RC7n8, 4.7 T, 5700 A,
Wire JE=680 A/mm2
t < 180 ms for limit
temperature < 300 K
Magnet current (A)
Protection time (s)
Time (ms)
Magnet voltage (Volt)

## Slide 9: Task 2. Improving quench detection for HTS magnets – quench detection made 2.6 s ahead of the state of the art method – hugely important for safety of HTS magnets
Time = 0 s
SCR opened
No ambiguity after -2.652s
No false detection to -3.096 s
No false detection from
-1000 s to -3.096 s
Staircase run with 30A/s ramp rate

## Slide 10: Able to have quench detection 2.5 seconds ahead, why it is exciting, and why this collaboration is interested and qualified to perform this work.
NEW LBNL QDS algorithm
Fast (discrimination at every 1 ms)
Work with all magnet operating scenarios
Implementable with FPGA.
To be applied, tested, and enhanced by US-Japan HTS magnets
- Test of KEK magnets at BNL
- KEK (CT0)
Currently also investigate machine learning for autonomous learning and anomaly detection (with Dan Wang, LBNL)
Front-end electronics
cRIO-FPGA
LabVIEW FPGA
User VI

## Slide 11: Our tasks
Task 1: HTS magnet technologies for high-radiation environment
  KEK, LBNL - Ceramic insulation, gamma-ray radiated epoxy resin composites, and neutron irradiation of REBCO tapes
Task 2: Stability, quench protection, and magnet safety
  Kyoto Uni., LBNL, BNL – quench modeling, experiments with single tapes and REBCO wires/cables.
Task 3: Measuring and modeling AC loss and field quality of HTS accelerator magnets
  Kyoto Uni., LBNL, KEK, BNL – magnets from C0 to C2, from modeling to experiments
Task 4: HTS/LTS high field hybrid accelerator dipole technology
  KEK – racetrack coils fab; BNL – test of KEK racetrack coils in 10 T background fields.

## Slide 12: Task 3. Kyoto Uni.: Effect of current-sharing on AC loss of CORC-like conductors and field quality
current
Dipole field
REBCO CORC Canted cosine theta dipole magnet demo
Test by Guangwei Xu, Kyoto Uni.. REBCO CORC CCT by Xiaorong Wang, LBNL, with ACT
C0, C1, and C2 have been constructed (Wang et al.,
10.1088/1361-6668/ab0eba; /10.1088/1361-6668/abc2a5
C3, 6-layer, 5 T CCT dipole magnet is ongoing.

## Slide 13: Future in the Accelerator Field
JPARC
NbTi Cable
  Ic (< 10 T) cannot achieve the requirement
Conventional Magnet Technology : Challenges
Neutron Target
MLF
Muon
Target
MLF 2nd Target Station
New Beam Line
Development of next-generation radiation resistant high field magnet
Organic Material for Insulation
  Degradation of the machine strength from 10 MGy
FCC@CERN: 100 TeV
  20 T high-field magnet
CERN
  Hilumi-LHC: 40 MGy (W-shield)
  FCC: >100 MGy?
J-PARC
  MLF2 : 130 MGy ?

## Slide 14: Task 4. KEK Inorganic Insulation of ReBCO tape
Continuous Coating of long ReBCO tape is performed using reel to reel coating machine
17
16
25
24
19
17
23
25
27
17
Successfully achieved
25 ± 4.7 (σ) μm thick ceramic coating.
Total Length : 40 m (Coated both sides)
Coating material: Al2O3:SiO2 = 1:1
Heat treatment: 100o C, 20 min
Withstand Voltage: 2 kV
Heat treatment
section
HTS reel
Automatic Spray
Winding the double pancake racetrack coil for high magnetic field test

## Slide 15: KEK HTS Coil – Winding and Test Status
Winding : Three coil with Coated ReBCO tape (wet winding)
The actual conductor thickness: 0.31 mm
(EuBCO: 0.16, coating layer: 0.05, adhesive layer: 0.1)
The number of turns: 20 turns
Winding setup for double pancake racetrack coil
Winding Completed
Preliminary tests at 77 K are undergoing at KEK
Extension support for HTS lead
Double Pancake HTS Coil
Extension support for HTS lead

## Slide 16: Overview of BNL Nb3Sn Common Coil Magnet Test Facility
Empty
Space
Insert Coil
BNL Nb3Sn common coil dipole DCC017 without insert coil
Structure for Test coil insert in Common coil
HTS coils inside Nb3Sn dipole - early experience of HTS/LTS hybrid dipole
Nb3Sn, common coil 2-in-1 dipole that allows two insert coils in two aperture
Structure is designed to provide a large open space (~30 mm X 335 mm)
New insert coils can be tested in the background field of up to 10 T (+ self-field)
Facilitates a rapid-turn around, low-cost R&D approach for high field magnets

## Slide 17: Upcoming Test Plan @ BNL, Upton
323.2
R5.5
Test Plan in July 2023 @BNL
Two HTS insert coils in two apertures of the common coil dipole:
Upper Bore: field primarily parallel
Lower bore: field primarily perpendicular
7 hall probes will be installed along the length to measure the magnetic field
Background
field :~10 T
29
29
Design study in undergoing in parallel
Field Quality studies will be undertaken at BNL
335
31

## Slide 18: Summary
Enable four institutions (LBNL, BNL, KEK, and Kyoto University) to team up to address critical issues facing high-temperature superconducting magnet technology for accelerator facilities.
Make possible progress and studies at both fundamental and technological fronts impossible with a single institution alone.
  Neutron radiation of REBCO tapes assisted with TEM studies.
  Quench protection of HTS magnets with new concepts, uncertain analysis with Monte-Carlo analysis, and quench protection with FPGA at much improved resolutions and margin of safety.
  LTS/HTS hybrid magnets.

## Slide 19: CCT magnet at LBNL and SCSC cable at Kyoto Uni.
LBNL C3 magnet

## Slide 20: Status of Neutron Irradiation
Irradiation study of Gd and other rare earth sample is undergoing
MASAMI IIO, KEK
M. Iio et al., IEEE Trans. Appl. Supercond., vol. 30, no. 4, (2020) 4600505.