## Slide 1: CMOS design for heterogeneous integration and future plans
Aikaterini Papadopoulou
Nanoscale hybrids Collaboration meeting

## Slide 2: Outline
Overview of past chip designs
Work plan

## Slide 3: 1. Envisioned device
A bio-inspired approach to imaging using color-sensitive receptors
Every photon is absorbed by one nanosensor or another depending on the color
Subwavelength nanosensors
A monolithic demonstrator pixel imager for
color-resolved single photon detection
Description
Goal
MICROELECTRONICS CO-DESIGN RESEARCH 3-YR AWARD
FOA: LAB 21-2491
Applications
Cosmology
Quantum key distribution/ secure communications
Single photon LIDAR
Biological imaging
Notes: Interdisciplinary effort - > good fit for Microelectronics Co-design research

## Slide 4: 1. Envisioned device
1. Silicon fabrication
2. Planarization
3. Oxide deposition
4. CNT deposition
5. Pd deposition

## Slide 5: 2. Passive array design
drain
source
Top metal with passivation opening
Top metal without passivation opening
gate
Test structures including ~90,000 sites for carbon-nanotube deposition designed in TSMC 180nm MPW
- Include padded-out terminals for standalone device testing, identification patterns, alignment marks

## Slide 6: 2. Passive array design comments
- How was the shape and geometry chosen?
- How was this used in the end?
- How to revise geometry?

## Slide 7: 3. Readout electronics
Designed in TSMC 180nm MPW
Includes standalone and integrated AFE with fixed-gain amplifier & output buffer. Specs based on past papers.
Standalone design successfully tested
Dies used for first development of post-processing steps
Block diagram of integrated readout IC
Simulation and measurement results of standalone amplifier

## Slide 8: 4. Initial attempts in post-processing
Post-processing requirements:
Controlled nanomaterials deposition requires a planar surface:
<10nm roughness
CNT diameter approximately 20nm
Desired gate oxide thickness under CNT approximately 20nm
Dies embedded in a 1” wafer for precision polishing
Height profile showing 3um topography before polishing
Chips polished to 50nm
flatness

## Slide 9: 5. TSMC 130nm full wafers
Migrate to TSMC 130nm in order to
demonstrate operation of a full
mini pixel array
Improved readout with higher bandwidth, programmable gain, higher input range, on-chip device biasing
Digital control and clock programmability for pixel array readout
Digital communication interface
New pad geometry

## Slide 10: 6. SkyWater 130nm full wafers
Nanotechnology Accelerator
Program
+
+
Wafer-level run with excellent 1nm planarity, and small 0.4um feature size
Design submitted in June 2023, including devices arrays and several variations of readout amplifiers

## Slide 11: 6. SkyWater 130nm new pad architectures
New tiny pad structures: - allow structure to fit into 25um AFM field - allow space around gate for hBN flakes
Experimental amplifiers

## Slide 12: 7. Work plans: preparation - accumulate feedback
- What have we learned from post-processing, oxide deposition, patterning etc.
- Feedback on shapes and geometries
- Feedback on placement

## Slide 13: 7. Work plans: preparation - modeling
No circuit design in first year
Get a model ready. Many levels of accuracy can be discussed: - IV curves from simulation -> Verilog-A LUT models - IV curves from measurement -> Verilog-A LUT models - IV data – Silvaco UTMOST software - If further interest – compact model tuning and development (photoresponse not modeled by any of existing models)

## Slide 14: Work plans: preparation - characterization
Most important: 1. Device testing and characterization
2. Chip testing and characterization