## Slide 1: CNT device fabrication and testing @ Sandia
Gaurang R. Bhatt
1/21/2025, LBL Meeting

## Slide 2
CNT-FETs - Refresher
Si
Drain
Source
Gate
CNT
Notes: Contacts – Ti/Pd..

## Slide 3
2% solution of CNT in toluene is spin coated
Average density 3-5 tubes/μm2
Deposition of CNTs
AFM
SEM

## Slide 4
Silicon
Silicon-MP
SWCNT
SWCNT
Raman

## Slide 5
CNT
Locating CNTs for making single-CNT FETs

## Slide 6
CAD preparation and locating CNTs: AFM image overlaid on CAD sub-field
AFM frame from Slide 9
CAD sub-field boundary

## Slide 7
Testing single CNT-FETs
Channel length = 100 nm
Notes: Low current
Contacts or surfactant residue are the suspected issues.

## Slide 8
FET noise measurement
Instrument noise floor
Vg = -5 V
Notes: 300 k ohm!

## Slide 9
CNTs on hBN

## Slide 10
CNT-FETs on hBN
Notes: Contacts are worse.. Metal not sticking on hBN

## Slide 11
Low noise FETs – WIP/Future plan
Instrument noise floor
hBN, Vg = -5 V
no-hBN, Vg = -5 V

## Slide 12
Low noise photon detectors – WIP/Future plans
Si
Drain
Source
Gate
Light absorbing molecule/atom
CNTs are poor absorbers of light by themselves.
Using QD/patterned TMDC to absorb light while CNT-FET provides a channel/mechanism for generated current

## Slide 13
CNTs
Slits
Integration with CMOS-WIP/Future plans

## Slide 14
Single SWCNT-FETs
Low noise photon detectors
Summary
Spin-on quantum dots
Patterned TMDC as light absorbers
Integration with CMOS
CNTs