## Slide 1: TMD Lithographic Synthesis
Towards CMOS compatible Integration
Tevye Kuykendall 1/21/2024

## Slide 2: Traditional synthesis of 2D Materials: Transition Metal Dichalcogenides (TMDs)
?
Exfoliation & Transfer
Chemical Synthesis (e.g. CVD)
Wafer-Scale
Fabrication
Transition Metal Dichalcogenides
MX2
M = Transition Metal
X = Chalcogen
Easy to learn and high quality materials. Not reproducible.
Reproducible materials. Non-trivial to define location and shape of materials.

## Slide 3: Lithographically Defined Synthesis of Transition Metal Dichalcogenides (TMDs)
A. Lateral Conversion: Microfabrication & Synthesis
B. Optical Microscopy (WS2)
H2
H2X
H2

## Slide 4: Lithographically Defined Synthesis of TMDs (cont.)
Cross-Sectional TEM of Various WOx Thickness
Cross-Sectional HRTEM
SiO2
WS2
Wafer Scalable
1 mm
Etched
area
Fully Converted
WS2
WS2 Raman Map
MoS2
MoSe2
WSe2
GaTe
20µm
PtxTey
MoTe2
WTe2
Sulfides
(H2S)
Selenides
(H2Se)
Tellurides
(Tellurium powder)
10 µm
WS2

## Slide 5: Lithographically Defined TMD Alloys & Heterostructures
Vertical Heterostructures
Lateral Heterostructures
Alloys
Cross-Sectional HRTEM
WS2
WS2
WS2
WS2
SiO2
SiO2
SiO2
WS2 - WSe2 (Optical Microscopy)
Raman Spectroscopy Line Scan
WS2
WSe2
WS2
W

## Slide 6
Lower growth temperature for CMOS compatibility?

## Slide 7
A. SiNx Membranes
Membrane
A. BCP patterning and liquid exfoliation transfer
Bottom
Top
Top
TEM to Study the Effect of Reduction and Growth Temperature

## Slide 8
Morphology trends
Grain Size
Crystallinity
Grain size:
Grain size:
9
Ref. *Marco D'Alessandro Master’s Thesis | 8
Notes: As you recall form the introduction - Reduction / conversion two step process, so a systematic study on the combination of them tells us morphology info. Interested to see how it behaves at low T to possibly integrate in CMOS tech which requires T around 400C maximum.
Here we have info on the impact of synthesis temperatures on the material. We can see from these images that higher T of reduction are associated to larger grain size and especially at 750 we have a coarsening of the metal producing large but discontinuous grains. Instead, at lower T the grains appear to be much smaller and also more continuous creating a more homogeneous material. This also affect the transfer resulting in a removal of the material improved.
Figure 3. TEM images of BCP patterned, laterally converted WS2, transferred to lacy carbon membranes. This shows the effect of H2 reduction, and H2S conversion on the morphology of the resulting WS2. The main images are bright-field, while the insets are dark-field. The illustrations on the left show the general trend in average grain size, and emphasize that the WS2 grain size was primarily determined by the reduction step of the synthesis.

## Slide 9
Morphology trends
Grain Size
Crystallinity
Grain size:
Grain size:
9
Ref. *Marco D'Alessandro Master’s Thesis | 9
Lower temperature conversion leads to lower quality TMD and gives limited conversion below 400C
Notes: As you recall form the introduction - Reduction / conversion two step process, so a systematic study on the combination of them tells us morphology info. Interested to see how it behaves at low T to possibly integrate in CMOS tech which requires T around 400C maximum.
Here we have info on the impact of synthesis temperatures on the material. We can see from these images that higher T of reduction are associated to larger grain size and especially at 750 we have a coarsening of the metal producing large but discontinuous grains. Instead, at lower T the grains appear to be much smaller and also more continuous creating a more homogeneous material. This also affect the transfer resulting in a removal of the material improved.
Figure 3. TEM images of BCP patterned, laterally converted WS2, transferred to lacy carbon membranes. This shows the effect of H2 reduction, and H2S conversion on the morphology of the resulting WS2. The main images are bright-field, while the insets are dark-field. The illustrations on the left show the general trend in average grain size, and emphasize that the WS2 grain size was primarily determined by the reduction step of the synthesis.

## Slide 10: Locally-Heated Chemical Conversion
Temperature, (oC)
0.2
0.5
1.0
Filament width (μm)
0.1V
c)
Simulated suspended heater
W
Si
Local conversion:
Precise patterning of TMD
Transfer-free method
High local growth temperature
Low substrate temperature
Device arrays allow parallel synthesis and automated characterization for application of AI/ML optimization

## Slide 11
Non-suspended device arrays for experimental design:
Establish proof of concept, conversion and characterization.
  Establishing fab processes for patterning (deposition/etching) tungsten filaments with ~50-100nm wire width.
  Chip carrier and device bonding for in-situ electrical testing
  Building/integrating electrical measurement hardware/software
  Tungsten filament conversion to WS2 using standard furnace heating to test characterization workflow (Eg. Raman, SEM, etc).
  Test first filament conversions (W -> WS2) using ohmic heating.
  Establish data workflow for large device array, “combinatorial” approach: Integrate with scope foundry for automation of Raman and SEM data collection.
Suspended devices
Outline of Experimental Plan

## Slide 12
5nm Ti / 250nm Au
50nm W
500-1000nm
50, 100, 200nm
50nm
Contact
Tungsten NW
2m
500nm

## Slide 13
Suspended devices
Provides improved thermal isolation of filaments. Less heating of CMOS, and enables higher conversion temperatures due to reduced conductive heat loss to substrate.
  A) Suspended devices on LPCVD SiN
    Establishing fab processes for patterning suspended filaments with ~50-100nm wire width on LPCVD SiN bridge.
    Testing, proof of concept, debugging.
    Device design for in-operando thermal measurement architecture.
    Prototyping and testing on non-CMOS architecture.
    Reduction of nanoribbon device dimensions using BCP
  B) Suspended devices on SiO2, SiN or other CMOS compatible bridge material
    Device design and integration on CMOS chips with thermal management.
Outline of Experimental Plan