## Slide 1: Silicon Tracking Detectors
Carl Haber
Physics Division
Lawrence Berkeley National Lab
chhaber@lbl.gov

## Slide 2
~ 4 mm (0.0001 m2)
~1975
~ 1 meter (200 m2)
~2005

## Slide 3
Suggestions for further reading
H. Spieler, Semiconductor Detector Systems, Oxford Science Publications, 2005
See also: http://www-physics.lbl.gov/~spieler/
G. Lutz, Semiconductor Radiation Detectors: Device Physics , Springer (July 11, 2007)
G. Knoll, Radiation Detection and Measurement Wiley; 4 edition (August 16, 2010)
A.S. Grove, Physics and Technology of Semiconductor Devices, (1967) John Wiley & Sons; ISBN: 0471329983
S.Sze, Physics of Semiconductor Devices, J.Wiley, 1981
T. Ferbel, Experimental Techniques in High Energy Nuclear and Particle Physics, World Scientific, 1992
W.Blum, W.Reigler, L.Rolandi, Particle Detection with Drift Chambers, 2nd edition, Springer, 2008
…and references therein

## Slide 4: Outline
Introduction to tracking
Semiconductor detectors
Signal processing
Sensors and architectures
Radiation effects
System issues – mechanics, power, metrology
Conclusions

## Slide 5: Tracking
The process of sampling a particle's trajectory and determining its parameters.
  Momentum, Direction, Decay points (kinks)
High energy
  Small fraction of energy deposited in instrument
Charged particles ionize matter along their path.
Tracking is based upon detecting ionization trails.
Trajectory is disturbed minimally by the process.
Here we focus on solid state detectors

## Slide 6: Track Parameters
Basic idea is a track curving in a magnetic field
3D track described by 5 parameters
p=momentum (or curvature in B field)
rip=distance of closest approach to the origin
f =azimuthal angle at the origin
zip= vertex along the beamline
q = polar angle

## Slide 7
z
y
x

## Slide 8: Tracker Characteristics
Parameters of the system
  geometry, layout, material, magnetic field, etc.
Performance of position sensing elements
  hit resolution, timing resolution, 1D/2D/3D
  Radiation damage effects
  defined by physics of detecting medium/process and general considerations such as segmentation and geometry.
Evaluation
  Initially evaluate with simple parametric analyses.
  Fast simulation
  Full simulation
  Bench, CR, and beam tests

## Slide 9
Simple case: Measure sagitta s of track with radius R, over projected arc length L (cm, KGauss, MeV/c), assuming R>>L
where Ds is the error on the sagitta measurement.
Effect of material: multiple scattering
s
Momentum Resolution

## Slide 10: Effect of Material
Minimize sagitta error
Maximize B,L
Minimize material

## Slide 11
for good resolution on angles (f and q) and intercepts (d, z0 )
Precision track point measurements
Maximize separation between planes for good resolution on intercepts
Minimize extrapolation - first point close to interaction
Material inside 1st layer should be at minimum radius (multiple scattering)
Vertex Resolution
Dx
x1
x2
y1
y2
a

## Slide 12
Point Resolution: Segmentation
Discrete sensing elements (binary response, hit or no hit), on a pitch Dx, measuring a coordinate x
Discrete sensing elements (analog response with signal to noise ratio S/N) on a pitch Dx, where f is a factor depending on pitch, threshold, cluster width
Dx
x

## Slide 13: 2D
The problem of 2 dimensions:
  90o array of n elements on pitch p: equal resolution on both coordinates.
    m hits -> m2 combinations with m2 – m false combinations
  Small angle stereo geometry, angle a
    False combinations are limited to the overlap region but resolution on second coordinate is worse by 1/sin(a)
Pixel structure: n x m channels
  Ultimate in readout structure
  Expensive in material, system issues, technology, cost
Pixels and strips are 2 extremes of a continuum (super-pixels, short-strips,…..)
  Could optimize performance vs. complexity but needs to be analyzed on a case by case basis

## Slide 14: Charged Particle Tracking Detectors
They rely on the “continuous” ionization of matter by fast charged particles
Energy loss/distance
  The minimum ionization approximation (MIP)
Signal formation process
Signal readout and noise

## Slide 15: Semiconductor Detectors
Since mid-80’s use of position sensitive solid state “silicon” detectors” became widespread
Can resolve track positions to ~several microns microns
Used to measure momentum and identify secondary vertices due to decays of primary particles
Handle high particle rates and radiation dose
Substantial commercial basis for technology

## Slide 16
Bandgap: leakage current
Dielectric constant: capacitance
Thermal conductivity: cooling
Radiation length: scattering
e/h pairs per MIP: signal
Mobility: speed
Displacement energy: damage
Breakdown field: HV stability
Ionization coefficient: gain mechanism

## Slide 17
Asymmetric diode junction: p(+) into contact with n, (NA >> ND) (can also have n+ in p)
Space charge region formed by diffusion of free charges, increased with "reverse bias“
Electron-hole pairs formed in the depletion zone drift under the influence of the electric field
Signal depends on width of depletion zone
Drift time determined by mobility and field
  ~7 ns to cross 300 microns
Drifting charge is a current which can be measured
Silicon Detectors
p+
n
V=0
VRB >0
W
p+
n
V=0
VRB > 0
e-
h+
h+
h+
e-
e-
n

## Slide 18: Silicon Microstrip Detector (Kemmer 1980)
Leverage microlithography and growing wafer scale to fabricate large position sensitive arrays → improved resolution on the mm scale, measure decay vertices
Strip pitch 50-100 mm

## Slide 19
Late 1970’s surface barrier
strip detector (Pisa)
~1980, 128 discrete channels
~14 mW/channel (CERN)
~1985, “Microplex”, 3 mW/ch
1st 128 readout ASIC,
1st application to colliding beams
(SLAC Mark II)
(Parker,Hyams,Walker)
Looking for charm in fixed target hadronic interactions…..b’s at lepton colliders….Higgs/BSM @LHC
6 mm
2020 RD53B
ATLAS
153,600 pixels
8 mA /pixel
20 mm

## Slide 20: Basic Formulae
= 0.5
~ 0.8 volts “built-in voltage”
Example: r = 5 KW-cm, VRB = 100 V, W = 354 mm
Signal is integrated charge
Noise is expressed as an
Equivalent input noise charge

## Slide 21: Signal Processing Optimizations
Signal increases with volume
Leakage current
  Decreases with lower temp and volume
  Increases with radiation and integration time
Noise
  Decreases with capacitance, leakage, power
  Increases with faster risetime
Generic no-name amplifier
Combination of rise and integration time
pre-amp
leakage

## Slide 22: 1st Order Correlations Between Sensor and Readout Electronics Characteristics
Dep\Indep | Volume | Radiation | Temp | Power | Leakage | Capacitance | Integrat. time | Risetime*
Signal | ↑ | ↓ |  |  |  |  |  | ↑
Leakage | ↑ | ↑ | ↑ |  |  |  |  | 
Input noise |  | ↑ |  | ↓ |  | ↑ |  | ↑
Shot noise | ↑ | ↑ | ↑ |  | ↑ |  | ↑ | 
Risetime* |  |  |  | ↑ |  | ↑ |  | 
Power |  | ↑ |  |  | ↑ |  |  | ↑
Required bias | ↑ | ↑ | ↑ |  |  |  |  | 
* Up means faster
Consider this as representative. The point is that a signal processing optimization should always be performed

## Slide 23
Finding top and bottom at the Tevatron ~1995…..

## Slide 24
2 m.
CERN ATLAS tracker (4th generation, beam in 2008)
CDF
1992

## Slide 25: Technology Roadmap
generation
year
luminosity
DT
chan/area
dose
readout
1
CDF SVX
1990
1029
3.5 ms
3.5 ms
128 ns
25 ns
25 ns
(30 ps)
50K/ 0.68 m2
25 Krad
3 mm CMOS
2
CDF SVX*
1995
1030
50K
100 Krad
1.2 mm RHCMOS
3
Run 2
2000
1032
600K / 5 m2
1 Mrad,
1013/cm2
0.8 mm
RHCMOS
4
LHC
2009
1034
5 x106 / 68 m2
108 pixels
10 Mrad 1015
0.25 mm CMOS
RH Bi-CMOS
5
HL-LHC
2025
5 x 1034
108 / 200 m2
109 pixels
100 Mrad
1016
65 – 130 nm CMOS
Commercial
6 Beyond HL/FCC
>2035
3 x 1035
25 ns
(5 ps)
5 x 108 / 400 m2
5 x 109 pixels
1-10 Grad
1018
Monolithic CMOS
4D, WBG materials

## Slide 26: Variations on the PiN Strip
HV deep N-well
P-well
NMOS PMOS
Depleted P-substrate
Not depleted
14 mm
@100V
P-well
Diode NMOS PMOS
Hi-Resistivity P-epi
P-substrate
N-well
N
Drift
Gatti and Rehak
Hybrid
Spieler, Nygren et al
Vertical
Monolithic Active Pixels (MAPs) Hi-Resistivity and HV

## Slide 27: LGADs
Reduce thickness
Add a higher doped gain layer
Collect primary ionization, multiply by gain, drift charge back across the thin drift layer
LGADs can provide time measurement with a resolution of ~30 ps
Require good S/N + fast rise
Present LGADs are ~mm2 future goal is ~50-100 mm2
But power may be excessive
n++/p+/p
n++/p
300 mm
50 mm
Si-LGAD
Metal
n++-type diode junction
p+ gain layer
p drift layer
LGADs are being installed in CMS and ATLAS to separate
pile-up events along the beam line

## Slide 28: 3D Sensors (S.Parker)
Implants are vertical
  Larger capacitance/pixel
  Requires special processing including MEMS technology
Collection distance is reduced
  Faster signal
  More rad-hard for CCE
Current applications to inner layers, beam monitors, timing
4.
4.
4.

## Slide 29: Alternate Materials
Very active R&D effort for >20 years
  http://rd48.web.cern.ch/RD48/
Most work has been on pCVD diamond material
  Significant improvement in charge collection
New results on single crystal materials – but small samples
Issue of industrial capacity vs silicon
New interest in energy technologies (batteries, electric transportation) has grown industrial focus on the large bandgap materials

## Slide 30
n++/p+/p
p++/n+/n
n++/p
300 mm
50 mm
Si-PIN
Si-LGAD
WBG-LGAD
75 mm
Few x 1012
~5 x 1014
75 mm

## Slide 31: Early Measurements of Gain in SiC
PiN @600V
LGAD @600V
LGAD @600V
PiN@600V

## Slide 32
Type | D | Timing | Fab | Cost | Application/Limitations/Comments
Silicon Strip p in n | 1 | ns | standard | $ | Basic, rad hard, outer tracking layers
n in p | 1 | ns | standard | $ | More rad hard, outer tracking layers
n in n | 1 | ns | double side | $$ | Partial depletion
Double sided | 2 | ns | double side | $$ | Radiation hardness issues with biasing
Silicon drift | 2 | Drift time | special | $$$ | Niche application to high multiplicity
CCD | 2 | Readout | boutique | $$$ | Slow, linear collider vertex
Monolithic Active Pixel | 2 | ns | commercial | $ | Large area, low cost, low mass
Hybrid Pixel | 2 | ns | combined | $$ | Hadron collider inner layers, bump bonded
Vertical Integration | 2 | ns | Sp. commercial | $$ | Advanced comm IC process, low mass
LGAD | 2* | ~30 ps | special | $$ | Fast timing by not yet high spatial resolution
3D Sensor | 2 | ~100 ps | very special | $$ | Fast, very rad hard, inner layers
HVCMOS | 2 | ns | commercial | $ | Fast, large area, in development, rad hard
High Resistivity CMOS | 2 | ns | commercial | $ | Fast, large area, in development, rad hard
Non- silicon |  | ns-30 ps | boutique | $$ | Diamond, SiC, etc, see DOE BRN report

## Slide 33: Readout Architectures
Experimental conditions, have, to some extent driven the development of a variety of readout architectures (see also the talk on ASICs/electronics)
Accommodate properties and limitations of available IC processes, a moving target
Subjective aspects have entered as well
Analog: process analog pulse heights off detector, full resolution, diagnostics, example is CMS APV25 series
Digital: digitize on detector, full resolution, examples are CDF SVX2-4 series, ATLAS pixel TOT system
Binary: on detector threshold, simplify readout, example is ATLAS ABC
Fast Timing is an emerging capability (few 10’s of ps)

## Slide 34: A Basic Collider Readout Architecture
Beam clock (BC) runs at collision rate, advances pipeline
Pipeline length determined by required latency
Trigger determines whether last cell will be read
Fast cluster read enables access to prompt data
25 ns
***
sensor
preamp
discr.
ADC?
pipeline
Compression
Cluster finding
Data readout
40
80
160
MHz
640 MHz
Fast cluster
read
trig

## Slide 35: One Example: Binary
Example is the ABC chip developed for ATLAS, BiCMOS
AC coupled pre-amplifier shaper for 25 ns collisions
Comparator + trim DAC per channel
1 bit pipeline clocked at 40 MHz, L1 buffer
Data compression
Control and configuration protocol
DSM CMOS version exists as well, 130 nm underway

## Slide 36: Radiation Environment
Primary source are collision products
  High energy charged particles + neutrals
Additional component due to “accidents”
Primary field falls with radius as ~r -(1-2)
Each interaction yields N particles/angular unit: sum crossings and interactions
Fluence and dose have increased >104 since mid-80’s
  At future colliders expect unprecedented dose due to increased luminosity and energy
    1-10 Grad absorbed energy (units)
    1015-1017 particles/cm2
    Compare to: space (~1 MRad), nuclear weapons (~1013)

## Slide 37: Radiation Effects: Ionizing
Incident particle interacts with atomic electrons
Measure in energy absorbed (rads (Si))
e/h pairs created, recombine or trap
Transient effect
  Actual signal formation
  Single event upset condition in circuits
Electronics: charge trapping at Si/SiO2 interface (largely controlled by rad-hard circuit designs or thinner oxides)
Detectors: surface effects, oxides

## Slide 38: Electronics
For systems up to the present - commercial rad-hard CMOS has provided sufficient resistance.
New chips use commercial deep submicron CMOS
  Thin oxides provide automatic hardness, verified in test
  Augment design rules with enclosed gate geometries to block radiation induced leakage paths
  Apply redundant circuitry to control single event upsets
Certain bipolar technologies are also rad-hard (analog)

## Slide 39: Radiation Effects: Non-ionizing
Incident particle interacts with nucleus
  Displacement damage – permanent or slow to reverse
  2nd order effects as defects interact over time
Depends upon particle type and energy
Measure in particles/cm2
Often expressed as “equivalent 1 MeV neutrons”

## Slide 40: Radiation Effects: Detectors
Damage to the periodic lattice creates mid-gap states
Increased leakage
  Shot noise
  Power
  Heat

## Slide 41
Reverse current with fluence and time

## Slide 42: Thermal Run-away
Power density mw/mm2
Increased current  Power dissipation Increased temperature Increased current

## Slide 43: Change in effective acceptor concentration
Effective space charge (Neff  Vfd) with fluence and time
Creation of acceptor states or removal of donor states
  Effective change of resistivity
  Type inversion: n  p
  Depletion voltage changes in proportion to |Neff| ’higher voltage operation required
  Dramatic time and temperature dependence

## Slide 44: Charge Collection
Reduction in charge collection efficiency (CCE)
  Ne,h(t) = N0 exp (-t/ttrap)
  Ratio of collection and charge trapping time constants evolves with fluence
Gregor Kramberger, Ljubljana

## Slide 45: Methods to Control Radiation Effects
Most represent some tradeoff
Size matters
  Smaller volumes generate less leakage current (but require more channels, power, heat…)
  Thinner detectors deplete at lower voltage (usually means less signal)
Temperature
  Low temperature (-40 C) operation can “stabilize” effective acceptor trend
  Reduce leakage current effects
Integration time
  Current noise is reduced for short shaping times at the expense of increased pre-amp noise, power.

## Slide 46
Biasing schemes
  Reduce value of parallel biasing resistor to reduce voltage drop due to ILeakRbias at the expense of increased thermal noise
HV operation
  Configure detectors to withstand higher voltage operation
  Tolerate increased depletion voltage
  Operate in partial depletion (collection issues)
Low noise electronics
  Tolerate reduced signal due to CCE and partial depletion
Configuration
  p in n substrate – simple, type inverts
  n in n substrate – 2 sided process, can be operated in partial depletion after inversion
  n in p – non-traditional process, does not invert (ATLAS upgrade)

## Slide 47
Strip detectors with multiple guard ringstructures to tolerate HV=500 V operation
Simulation of 10 year operating scenarios
for silicon tracking at the LHC
L= 1033-1034

## Slide 48: Issues for Systems
Packaging and interconnections
Grounding and Shielding
Powering and Bias
Control and Data Transmission
  Cables
  AC Coupling
Monitoring and fast/slow control
  Interlocks, safety
Mechanical Support and Cooling
Scaling of Assembly
Metrology

## Slide 49: Electrical Materials
material | Resistivity (mWcm) | Dielectric constant | Xo(cm) | Thermal C. (W/moK) | CTE (ppm) | Young’s Module (GPa)
Silicon |  | 11.9 | 9.37 | 149 | 2.6 | 135-185
Aluminum | 2.65 |  | 8.9 | 237 | 23.9 | 
Copper | 1.67 |  | 1.43 | 398 | 16.6 | 
Gold | 2.44 |  | 0.335 | 297 | 14.2 | 
Carbon | 1375 |  | 19.32 | varies |  | 
Kapton |  | 3.4 | 28.4 | 0.2 | ~20 | 
SiO2 |  | 3.9 | 10 | 1.1 |  | 
BeO | 1021 | 6.6 | 14.4 | 230 | 8.3 | 331-400
AlN | >1020 | 9 | 8.4 | 170 | 4.3 | 202-346
Al2O3 | >1020 | 9.0 | 7.55 | 24 | 7.2 | 215-413
G-10 |  | 4.7 | 19.4 | 0.2 |  | 

## Slide 50: Circuit Board Technology
Subtractive process – use chemical etch to define conductors
Additive process – print conductors, insulators, and passive components
  Higher performance substrates are available

## Slide 51: Emerging Subtractive Processes

## Slide 52: Packaging and Interconnections

## Slide 53: Power Distribution and Bias
Conventional wisdom stated that each “module” of tracker should be serviced independently
  isolate single point failures
  Avoid electrical interference and ensure low noise
For large trackers this has led to a cabling (mass and access) limitation
Future trackers are larger by x5 or more
An active R&D effort in alternative powering approaches resulted in a major revision of this orthodoxy
Now alternative powering schemes are in wide use with significant material and cabling reductions as a result
Also HV multiplexing with rad hard switches
Sophisticated monitoring and control ASICs – ATLAS AMAC, PSPP

## Slide 54
Independent powering
Serial powering
DC-DC powering
Hybrid current = I
Number of hybrids =n
Total current = nI
Power lines = n
Hybrid current = I
Number of hybrids =n
Total current = I
Power lines = 1
……
Constant
current
source
Constant (high)
voltage
source
Hybrid current = I
Number of hybrids =n
Total current = n(I/R)
Power lines = 1
……
……
1
2
3
4
5
6
n-1
n
1
2
3
4
5
6
n-1
n
1
2
3
4
5
6
n-1
n
……
+
-
Requires AC coupling
Vtot = N*Vmod
Shunt regulation
Equal I per module
Requires clocked
stepdown converter
per module
Inductor
Vin=Vmod*R

## Slide 55: Implementations
30 drop
Serial powered
Stave
HV multiplexers
DCDC Converters
ATLAS HL-LHC Module with DCDC,
HV-mux, monitoring and control ASIC

## Slide 56: Data Transmission and Electrical Services
Required services
  Clock/Control/Data – fast, controlled impedance
  Slow control and monitoring
  Power/ground/bias
Lowest mass electrical = flex circuits
Controlled impedance strip lines
Sufficient copper to control voltage drops

## Slide 57: Mechanical and Thermal Aspects
Precision tracker requires support structure which is stable, can be efficiently cooled, and is low in mass (Xo).
There are two key materials/classes which come into consideration here
  Beryllium: structural grade metal, low Z, metallic CTE, expensive, and hazardous to machine, probably impractical for very large structures
  Carbon composites: tremendously flexible class of materials, reasonable Xo, good thermal properties, variable CTE
Many advanced implementations now favor integrated carbon composite structures ie: staves, I-beams, tubes…
Flow of liquid coolants – initially fluorocarbons, now CO2, air cooling for very low mass systems - MAPs

## Slide 58: Mechanical Grade Materials
material | Density (gr/cc) | Xo (cm) | Young’s Mod (GPa) | CTE (ppm/oK) | TC: W/moK
Silicon | 2.33 | 9.37 | 130-185 | 2.8-7.3 | 149
Beryllium | 1.85 | 35.27 | 255 | 12.4 | 201
Aluminum | 2.70 | 8.9 | 69 | 23.9 | 237
Stainless Steel | 7.9 | 1.76 | 193 | 11.7 | 95
Titanium | 4.54 | 3.56 | 116 | 8.5 | 
Carbon | 2.21 | 19.32 |  | 0.6-4.3 | 
Carbon fiber frac 70-40% | ~1.7-2 | 23-27 | 180-125 along fibre | Varies with layup | 10’s – several 100’s
CF: K13D2U | 2.2 |  | 135 Msi |  | 800
POCO Graphite foam | 0.5 | ~100 | low | 0.7 | 45/135 in/out
Boron Nitride | 2.25 | 20.8 |  | <1 | 250-300

## Slide 59: Carbon Composites
Carbon fiber “sheets” consist of filaments or woven layers impregnated with epoxy = “pre-preg”.
By arranging layers in various “lay-ups” and configurations, a variety of components are created with enhanced mechanical and thermal properties.
Importance of symmetry and stress balance
Other advanced carbon based materials can be combined in structure as well
Multiple shapes and materials can be simultaneously co-cured
Modules are on “local supports” which are then placed on “global supports”

## Slide 60: Basic Issues
Sag in a uniform composite beam
Stress in the “bi-material” strip
b
h
c
t
t

## Slide 61: Example: Carbon Fiber Beam
Structure consists of 2 CF facings laminated on either side of a “soft” core w. embedded metal cooling lines: sandwich beam
Symmetry keeps the structure flat
Facing contains multiple sheets in order to tune mechanical and/or thermal properties
Core may have enhanced thermal properties to improve cooling efficiency
Subsequent (or co-)lamination of electrical circuitry and sensors
Issue of stress between carbon and other unlike materials as composite is cooled from lamination temperature to RT and to operating temperature

## Slide 62: ATLAS I-beam Structures
Typically a cured (or co-cured) structure composed of fibers, a polymer matrix, additional elements such as foam, honeycomb, embedded cooling channels, electrical interconnects
Low mass CF structure/specialized materials
Embedded thermal aspect, thin walled pipes, engineered interfaces
Embedded electrical functions

## Slide 63: Materials: Carbon Foams: Low density, hi conductivity
Developed in collaboration with industry through SBIR
Qualified for radiation tolerance and thermal/mechanical performance, in use.
FEA modeling of thermal and mechanical properties.

## Slide 64: Composites Facility

## Slide 65: Metrology Tools for Survey
Technology | Application | Resolution | Interface | Ease/Speed
CMM-touch | Large objects | x/y/z ~ mm’s | commercial | Teach mode
CMM-optical | In plane location Small heights | x/y/z ~ mm’s | commercial | same
ESPI | Dynamics | x/y/z ~ mm’s | commercial | R&D tool
FSI | In-situ alignment Stability | One axis | custom | System design
Laser Displacement | Flexible heights R&D tests | z ~ mm’s | User defined | User defined, 1 KHz
Structured Illumination | Fast large area 3D | x/y ~ mm z ~ 0.2 mm | Video or still camera | Typical frame rates
Confocal | Precision heights Small area | 10-100 nm | User or commercial | User defined, 100 Hz–2 KHz

## Slide 66: Examples
Touch/Optical Coordinate
Measuring Machines
Image analysis
Structured
Illumination
Scanning Laser
Rangefinding
Triangulation
Electronic Speckle Pattern Interferometry
Color Coded or Laser
Confocal Microscopy

## Slide 67: Example: ATLAS Strips Stave for HL-LHC
For HL-LHC upgrade “ITk”, ATLAS chose to mount groups of modules on a “local support” structure referred to as a “Stave”
Front load assembly/test, integrate support/cooling/services

## Slide 68: Modular Architectures

## Slide 69: Bad: Stress/Vibration Induced Electronic Noise
Scan of backside of sensor at -60C
Powerboard
~1 cm
Vibrations confirmed using a laser doppler vibrometer.
  Amplitude: 𝒪(10 pm) - 𝒪(1 nm).
  Frequency: 2 MHz → driven by DC-DC converter switching
Ultimately cured by interposing a layer of soft adhesive gel under
the hybrids and powerboards…

## Slide 70: Realized Systems - Packaging
ASICs → Custom Packaging
PCB and flex, controlled Z
Materials
Radiation
Thermal management
Precision Assembly ~ few mm
COB
Interconnections
1.4 m
10 cm
100 mm lines

## Slide 71: Challenges for the Future
Concepts for a future colliders focus on two branches
  A e+e- collider based Higgs Factory: high precision tests of the SM
  A 10 TeV parton CMS energy frontier collider (10x LHC) either proton or muon
  CERN envisions this as a sequential program using a new 100 Km circular tunnel
Challenges for a Higgs Factory
  Very low mass
  Control of systematic errors
Challenges for a 10 TeV parton CMS collider
  4D tracking: large multiplicity, multiple interactions/crossing
  High radiation resistance

## Slide 72: The Future of Particle Detectors
In 2019-20 the Dept of Energy Office of High Energy Physics requested a community study of needs for transformational instrumentation R&D for future HEP experiments. Report released Aug 2020
https://science.osti.gov/hep/Community-Resources/Reports
See also ECFA Detector R&D Roadmap: https://cds.cern.ch/record/2784893
Basic Research Needs for High Energy Physics
Detector Research and Development
Led by
Ian Shipsey and Bonnie Fleming
Our colleague Ian Shipsey passed away on
October 7, 2024. These lectures are dedicated to him.

## Slide 73: Future Detector and Electronics Challenges
Extremely low mass to enable high precision measurements
  Ultra thin (~50 microns) sensors and electronics
  Data transmission: low mass, high speed links
  Power management: high efficiency to reduce material and losses, innovative cooling schemes
  Possibility to operate at high temperature
Precise knowledge of detector performance – acceptance, efficiency to control systematics
Local intelligence: capable of compressing data in real time to reduce BW
Granularity/Timing: fine grained pixelated sensors ~50 mm2, fast timing with 10-100 ps resolution, covering several m2 - ~100 m2 (albeit with less granularity)
Radiation hardness: relates to the future of the LHC and FCChh, requiring sensors which can sustain up to 1017 1 MeV neq, and electronics which can absorb up to 10 GRad.
Integrate new technologies – advanced node, WBG, thin films, nano, Si photonics
Integrate new tools and components/capabilities

## Slide 74: Conclusions
Huge progress ~30 years to build silicon trackers using a broad suite of advanced technologies
Much significant science done, and to be done, with these devices
R&D underway for the next generation

## Slide 75: Back Up Slides
Front End Architectures
Fast Cluster Finding Architecture
Thermally enhanced materials
Newer processes
Electronic Packaging
Production Lines

## Slide 76: Signal Processing Issues
Signal
  Energy loss by particle in Si
  Proportional to thickness (volume)
  Radiation can affect charge collection efficiency
Leakage current
  If DC coupled then must be compensated by filter, feedback, or injection
  Before (after) LHC radiation damage ~ 1 nA (1 ma)
  AC component is seen by pre-amp: noise source
Input Noise
  Preamp “input noise charge”, white noise, decreases with pre-amp current, increases with faster risetime
  Bias resistor: source of thermal noise
  Radiation activated

## Slide 77: Double Correlated Sample and Hold
Original MOS monolithic architecture, no resistors
High frequency bandwidth limited by pre-amp
Low frequency limited by DT=T2-T1
Can be generalized to N samples but incurs a noise penalty factor of √2 for each pair

## Slide 78: Analog
Example is the APV25 chip developed for CMS
Readout all analog pulse heights, no sparsification
Dual function: fast time mode, slow low noise mode
Utilize analog signal processing on-chip to measure pulse time

## Slide 79: Digital
Example is the SVX4 chip developed for CDF
Switched capacitor analog pipeline
Combined analog threshold + 8 bit digitization
Sparse readout

## Slide 80: Binary
Example is the ABC chip developed for ATLAS, BiCMOS
AC coupled pre-amplifier shaper for 25 ns collisions
Comparator + trim DAC per channel
1 bit pipeline clocked at 40 MHz, L1 buffer
Data compression
Control and configuration protocol
DSM CMOS version exists as well, 130 nm underway

## Slide 81: ATLAS Pixel
Example is ATLAS FEI3 pixel cell
DC couple preamp with leakage current compensation
Pulse height is measured by “Time over Threshold”
Additional architecture organizes the data in columns for readout

## Slide 82: Variations on the Strip Detector
Silicon drift detector
Double sided detector
p+ in n
n+ in p
n+ in n

## Slide 83: Pixel Detectors
CCD
Charge Coupled Device
Relatively slow
Low noise, Low mass
Monolithic Active Pixel
electronics and charge
formation/collection in a
thin epitaxial layer, diffusion
Moderate speed
Low noise, Low mass
Hybrid pixel
FE IC and sensor joined
by a bump bond
Fast,Radiation Hard
Most widely used now

## Slide 84
Real time momentum trigger
Horisberger
See WIT2010,12,14
pub in JINST
This concept has been
developed into a full scale
tracker architecture by the
CMS collaboration for the
HL-LHC. See their TDR
https://cds.cern.ch/record/2272264/files/CMS-TDR-014.pdf
The ATLAS collaboration
has studied, but will not use,
a more limited version of this

## Slide 85: Fast Cluster Finder
Normal operation
  Beam clock advances FE pipeline
  Readout clock at beam clock rate or more pushes data out for full readout
Possible to do a fast internal search for a limited number of clusters (hits)
Read these out on dedicated lines at hundreds of MHz
Sufficient to supply 2x16 bit addresses per BC which is OK for <1% occupancy, more for

## Slide 87: Example: Thermally Enhanced Materials Survey
Carbon NanoFiber
Synthetic graphite
Natural graphite
Thermal Conductivity [W/mK}
0 0.5 1 1.5 2 2.5 3 3.5 4
0 5 10 15 20 25 30 35
Filler Content [vol %]
Loading of epoxy or other adhesives
Typical materials in present use for HEP: 1-1.25 W/mK
Can improve by x >2…

## Slide 88: New developments
Engineered materials
New configurations, 3D electrodes, interleaved strips
Cryogenics
Alternate materials: Diamond, SiC,…
RD efforts organized at CERN
  RD42: development of diamond as detector
  RD48: radiation damage to silicon
  RD50: development of radiation resistant detectors
  RD39: cryogenic detectors and systems
  http://rdXY.web.cern.ch/rdXY

## Slide 89: Engineered Silicon
Microscopic understanding of damage mechanisms, defects, and kinetics
  Modeling
  Measurements
  Time and temperature dependence
Engineer the silicon for greater radiation resistance

## Slide 90
Harris Kagan
http://rd42.web.cern.ch/RD42/

## Slide 91: Cryogenic operation
Palmieri et al (1998) recovery of lost CCE at cryogenic temperatures
“Lazarus Effect” due to freeze-out of traps
R&D activity centered at CERN (RD39)
Practical difficulty for “low mass” tracker if substantial cryogenic engineering and infrastructure is required.

## Slide 92: High Density Packaging
Electronic packaging is often the only “reducible” part of the detector mass
Advances in packaging have allowed us to integrate increasing complexity into denser footprints
Maintain necessary thermal performance with minimized mass and high reliability
Key technologies are based upon commercial processes
Avoid the homemade syndrome

## Slide 93: Key Technologies
Surface mount technology (SMT), pick & place
Flexible circuits
High density multilayer PCB and flex
  Trace widths/space approaching 25 mm
Large area flexible circuits > 1 meter length
Chip on Board (COB) and Chip on Flex
Thin film on ceramic, glass, and polyimide
Thick film on ceramic, BeO and AlN substrates
Lamination onto high-TC carbon substrates

## Slide 94: Technology examples

## Slide 95: Wirebonding
Mainstay of microelectronic interconnection
Typically uses 25 mm Al or Au wire, ultrasonic welding process
Requires particular control of materials, cleanliness, and process
Automated (5 bonds/sec) machines are commercially available and in widespread use in the HEP and related communities
75 mm pitch is achievable with good process control, a typical HEP “module” might contain ~5000 bonds

## Slide 96: Bump or Flip Chip Bonding
Wirebonding is impractical for large 2D arrays
ATLAS pixel cell is 50 x 250 mm
At this density FE interconnect is made with a conductive “bump”
This is an industrial process and requires expensive technology, therefore has not become “in-house”
Xray of bumps
16 chips. 46,080 bump bonds
Sensor (below)
ICs
6.3cm
2cm

## Slide 97: Bump Bonding Processes
SOLDER BUMPING
INDIUM BUMPING

## Slide 98: ATLAS ITk Strip Tracker Stave Structure
400 staves, 1.4 meter, 28 10x10cm silicon modules, DCDC power

## Slide 99
Tape inspection
layup
Lamination
Co-cure
Thermally enhanced
materials
Plasma clean
Wirebond
Precision assembly + metrology
Module
assembly
wirebond
Hybrid
assembly
inspection
FE IC
sensor
Power Board +
components