## Slide 1: Picosecond timing resolution with scintillators for a new generation of HEP detectors and Time-of-Flight PET scanners
Paul Lecoq
CERN, Geneva
This work and presentation are made
in the frame of the ERC Advanced Grant Agreement N°338953–TICAL
Notes: Stefan: Paper ID: #2558 Title: Systematic assessment of novel scintillator and SiPM technologies for highest TOF resolution in PET and HEP Session: N-25, 'Scintillation Detectors I’
Poster panel (face) ID: 19 Poster Number: M-03-019 Paper ID: #1605 Title: Impact on the time resolution of double sided crystal readout in TOF-PET Session: M-03, 'Poster'
Julien Rossignol: Paper ID: #2617 Title: Time-of-Flight Computed Tomography: Proof of Principle and Challenges Session: M-06, 'MIC Plenary 3: IEEE NPSS Christopher J Thompson Student Award Finalists’
Rosana: Paper ID: #1150 Title: Timing performance of a two-active material sampled pixel: LYSO plates coated with CdSe/CdS nanoplatelets Session: N-25, 'Scintillation Detectors I’
Paul&Rosana: Poster panel (face) ID: 4 Poster Number: M-03-004 Paper ID: #1291 Title: A Metamaterial approach in the frame of the 10ps Time-of-Flight PET challenge Session: M-03, 'Poster'

## Slide 2: Why fast timing?
1/5 sec
1/500 sec
1/5000 sec

## Slide 3: Why 10ps timing resolution
Time-of-Flight techniques to alleviate the pile-up problem and help improving energy resolution at high luminosity colliders
Improve resolution of finely segmented homogenous calorimeters
Time-of-Flight PET sanners with > 10 fold improvement in sensitivity
CT X-Ray imaging
Imaging in turbid media
hyperspectral time resolved spectroscopy for high precision dynamic studies of fast phenomena
Notes: HEP ... because we are looking at very rare events and to produce only a few of them we need to use high luminosity colliders, with a huge number of uninteresting collisions
Need for X-Ray and hyperspectral time resolved spectroscopy ...
also because there is a demand for a 10 fold increase in molecular imaging sensitivity and TOFPET can allow this

## Slide 4: Detection of ionizing radiation What matters?
Where
Energy
Particle ID
When
TOF
Finely segmented
calorimeters
Notes: Link time ID (Finely segmented Time Imaging calorimeter) and time spatial localisation (TOF)
We see now coming a growing request for better timing resolution, boosted by emerging technologies opening the management of time at the ps level.

## Slide 5: HEP Principle of pile-up mitigation
Use the tracker to determine the z position
of the vertex (large angle tracks)
Use TOF to associate a time to a vertex
For a luminous region distributed
over ~ 10cm, collisions will be
distributed over ~ 300ps
Requires 10ps timing resolution !!!

## Slide 6: HEP: CMS timing layer
248’832 LYSO/SiPM
The CMS Collaboration, Technical Proposal for a Mip Timing Detector in the CMS Experiment Phase 2 Upgrade, CERN-LHCC-2017-027 ; LHCC-P-009
Notes: And we are now discussing a new generation of detectors, like the timing layer of the CMS upgrade (scheduled for 2020), and which requires very fast and high gain photodetectors and which will use a quarter of a million SiPMs

## Slide 7: CMS timing layer: beam tests with mip’s
≈ 5 MeV
≈ 3 MeV
A.Benaglia, M. Lucchini et al., NIM 830 (2016) 30
≈ 3 MeV
30 ps
Smaller SiPM / crystal area coverage

## Slide 8: Hadron energy deposition in a segmented hadron calotimeter
50GeV proton in a 1x1x3m3 iron block
segmented in 1mm thick layers
About 1 MeV/mip/layer
Global time t
Local time t-z/c
A. Benaglia, E. Auffray, P. Lecoq, H. Wenzel, A. Para, IEEE Trans. Nucl. Sc. VOL. 13, NO. 9, Sept. 2014
Notes: Precise timing in one or more EM? HAD? Calorimeter layers to associate jets with primary vertex (TOF) and reduce pile-up
Use timing information to help PFA association and to reduce the confusion term
Use event-by-event space-time evolution of energy deposition to improve the energy resolution

## Slide 9: Dual Gate (scintillation) vs Dual Readout (Scint. + Cher.)
A. Benaglia, E. Auffray, P. Lecoq, H. Wenzel, A. Para, IEEE Trans. Nucl. Sc. VOL. 13, NO. 9, Sept. 2014

## Slide 10
Detector B
Detector A
e-
e+
Patient
tA
tB
Dt = tA – tB = [(d+d1) – (d-d1)]/c
d1 = c Dt/2
d
d1
Time of Flight PET
dt (ps)
10
100
300
500
dx (cm)
SNR*
0.15
1.5
4.5
7.5
16
5.2
3.0
2.3
* SNR gain for 40 cm phantom
SNRTOF = √(2D/cDt) · SNRconv
10ps TOF resolution
dx = 1.5mm
SNRTOF/SNRCONV= 16!
State-of-the-art
Notes: But there is also a request for good timing resolution for another important application of scintillating crystals. PET scanners.

## Slide 11: Why 10ps TOFPET?
TOF for direct 3D information
  Requires 10ps TOF resolution for 1.5mm resolution along LOR
Allows limited angle tomography without artifacts
> 15-fold improvement in S/N ratio, even more with high random rate
  Equivalent potential in dose reduction (0.5mSv/scan)
    Annual natural background: 2.4mSv
    Return flight Paris SFO: 0.11mSv
  Allows longer longitudinal studies per injection
  Reduce the cost of radiotracer production infrastructures
Less sensitive to incorrect attenuation correction and normalization
  Less stringent requirements on CT: cost, dose reduction
  Reduce problems of not direct attenuation measurement in PET/MR
Open PET to new categories of patients (children, fœtus)
10ps TOFPET
Conventional PET
Current state of the art for PET commercial devices: 500-250ps
Current state of the art in the lab: 60-100ps (3-20mm crystals)
Notes: - 10ps resolution correspond to 1.5mm resolution along the LOR and opens the way to reconstructionless PET
- this would considerably reduce the constraints associated to the tomographic principle, which requires full angular coverage of the ROI, and allow limited angle tomography without artifacts
- 10ps resolution would bring a > 15 fold ...

## Slide 12: Where are we today for PET?
S. Gundacker et al, 2016 JINST 11 P08008
Measured with FBK NUV-HD (25μm SPAD size, 4x4mm2 device size)
2x2mm2 crystal cross section, T=15°C
30%
44%
NINO
Breaking news
HF electronics
58ps
98ps
Notes: In red assume LTE =100%
In green: influence of LTE
In Yellow: influence of PTS

## Slide 13: The detection chain
q2
SiPM
Crystal
electronics
g
Dt
tkth pe =
Dt
Conversion depth
+ tk’ ph
Scintillation
process
+ ttransit
Transit time
jitter
+ tSPTR
Single photon
time spread
+ tTDC
TDC
conversion time
Random deletion 1
Absorption
Self-absorption
Random deletion 2
SiPM PDE
Unwanted pulses 2
DCR
Unwanted pulses 1
DCR, cross talk
Afterpulses
How to extract the
best time estimator
from the signal?
Notes: I will show again this slide that I have prouced several years ago, and which ihas become very popular.

## Slide 14: Classification of scintillators
Ideal
Scintilllator
Notes: The Quest for the ideal very dense, very bright, very fast scintillator is going on.
But can we have a scintillators with 10 times higher LY and 10 times faster decay time than LSO?

## Slide 15: Prompt photons to boost the timing resolution
Cramer Rao calculations including photon transfer time spread (PTS) and light transfer efficiency (LTE) of a 2x2x3mm3 LYSO:Ce ,Ca crystal, glue-coupled to a 4mm2 FBK-NUV HD SiPMs with 40um SPAD size
S. Gundacker, CERN
Notes: The pDE being already quite high the factor on which to play is the SPTR

## Slide 16: Possible sources of prompt photons ( < 1ns)
Ce3+ Activator: 5d-4f
Ca2+ & Mg2+ co-doping
τr ~ 20 ps τd ~ 16 ns
Cerenkov
τ ~ 5-10 ps
Cross Luminescence
<1ns
<300 nm – low LY
Hot Intraband Luminescence
0.1 - 10 ps
Excitons/Bi-exciton
stable at 300 K
High donor band semiconductors <1ns
quenched at room temperature
Notes: Cross luminescence. Very fast but not taken too seriously so far because of a relativelylow LY and an emission in the UV. But this situation can change with the development of new solid state photodetector with a QE as high as 20% @ 200nm.
High donor band semiconductor, introduced by Lehman in 1966 with ZnO and CdSe, and reactivated by S. Derenzo and M. Weber in 2002 with PbI2, HgI2, CuI

## Slide 17: LSO:Ce,Ca / BaF2
Eg
hν
Crossluminescence
1400ph/MeV
600ps
220nm
50
s
Glue coupling: LTE = 68%
50
s
Air coupling: LTE = 35%
S. Gundacker, CERN
Courtesy of Hamamatsu
Notes: SPTR in sigma
LSO:Ce:0.4%Ca scintillator to 4x4mm2 FBK NUV-HD SiPMs with 40m m SPAD size
BaF2 air coupled to SiPM Hamamatsu VUV (S13370) 1400ph/MeV 600ps 220nm

## Slide 18: Hot intraband luminescence
The small energy relaxation rate below the ionization threshold leads to:
  a high density of optical and acoustic phonons
    local heating, shock wave, transient absorption
  a dynamic e population change from the top to the bottom of the conduction band
If the density of states is not uniform in the conduction band a competition can take place between phonon mediated non-radiative relaxation and radiative relaxation between conduction sub-bands
Notes: See Cs2CdI4 paper Pidzirailo
Alos list of crystals propsed by Oimelkov and Vasiliev

## Slide 19: Hot intraband luminescence
Ultrafast emission ≤ 10-12s
  e-IBL: broad spectrum in visible range
  H-IBL: NIR psectrum
Independant of temperature
Independant of defects
Absolute Quantum Yield
  Whn/Wphonon = 10-8/(10-11-10-12)
  ≈ 10-3 to 10-4 ph/eh pair
Higher yield if structures or dips in CB? Interesting to look at CeF3
Omelkov et.al., J. Lum., 176 (2016) 309–317
Notes: Vaisburd,.Evdokimov, phys.stat.sol.(c)2(2005)216-222
If we can manage to have a non uniform density of electron states in the conduction band (symetrically of holes in the valence band) we can have a competition between phonon assisted non radiative relaxation and photon assisted radiative recombinations

## Slide 20: Search for Candidates for Hot intraband luminescence
Search for materials with splitting of the conduction/valence band
Search for materials with flat sub-bands for a perfect delocalization of the electrons/holes
  Examples Oxy-halide compounds
Ba4OF6 4.61g/cm3
GdOF 7.51g/cm3

## Slide 21: Cerenkov contribution
LuAG:Ce
LuAG:Pr, Ca
S. Gundacker, E. Auffray, K. Pauwels, and P. Lecoq, Phys. Med. Biol. , vol. 61, pp. 2802–2837, 2016.
LuAG:Pr
0,28%
3,4 Cerenkov photons

## Slide 22: Lowering Cerenkov threshold ?
Cerenkov threshold (101keV in LSO) can be strongly lowered (↘100’s eV) in specifically designed nanostructured metamaterials
Related more formally to the Smith Purcell effect
  A kind of Cerenkov or transition radiation emission ➝ free electron lasers
Produce constructive interference of resonance transition radiation (plasmonic states) in photonic crystals
  !! No velocity threshold !!
Y. Yang et al., Nature Phys. Lett., 16 July 2018
I. Kaminer et al., Nature Comm., 13 June 2016
Notes: Also Smith–Purcell effect (at the basis of free electron lasers): Essentially, this is a form of Cherenkov radiation where the phase velocity of the light has been altered by the periodic grating. a is periodicity m diffraction order.
Transitionm Radiation: a form of electromagnetic radiation emitted when a charged particle passes through inhomogeneous media, such as a boundary between two different media.
Free electron lasers: coherent emission has been observed with e energy as low as 250eV
Engineering of a metamaterial with low permittivity to reduce the phase velocity. The plasmonic-polaritons on the surface produce constructive interferences of the resonance transition radiation

## Slide 23: Lowering Cerenkov threshold with hyperbolic metamaterials
kz
kx
kz
kx
k+
k-
Slow e-
Fast e-
Isofrequency contour from dispersion formula: k
Isofrequency contour from dispersion formula: k
k-
k+
for isotropic dielectric material
Finite density of photonic states in dw
+ +
for anisotropic hyperbolic material
Infinite density of photonic states in dw
+ -
M. Silverinha, Nature Photonics, Vol. 11, May 2017
Notes: In isotropic dielectric materials only fast electrons, associated to short transverse wavevectors can couple to photonic states k+ and k-
HMM: Nanostructures having dielectric properties in some directions and metallic properties in other directions.
Originally introduced to overcome the diffraction limit of optical imaging
Number of interesting and unusual properties due to their high density of photonic states
Photonic hypercrystals combine the most interesting features of photonic crystals and hyperbolic metamaterials
HMM are a fantastic playing field, which starts to be successfully exploited in photonics, and in photovoltaic, but which has not entered yet our domain of radiation detectors. Its potential is huge, only limited by our imagination.

## Slide 24: Multi-exciton quantum confinement
X
Gx
XX
Gxx= 4Gx
XXX
Gxxx= 9Gx
Padilha et.al., Nano Lett. 2013, 925-932
CdSe/ZnS
tx ~ 1ns
txx = 196ps
txxx = 69ps
Notes: Padhila, Klimov, Nano lett 2013, 13, 932-932 Response of NCs to high energy excitations
Fortunately the excitation density is high due to the very inhomegeous dE/dx energy deposition of the recoil electron

## Slide 25: GOS in 1D quantum confined systems
LYSO plate 200mm thick
+ CdSe/CdS nanoplate film 20mm thick
J.Grim, I. Moreels
ITT, Italy
372 nm laser or X-rays
Streak
Camera
Focal spot
LYSO
200mm
20mm CdSe film
deposition
optical
table
R. Martinez Turtos et al., JINST_068P_06
530nm
530nm
420nm
Notes: Left: Streak focussed on CdSe: Fast peak from laser excitation of CdSe. Long tail CdSe excitation by LSO scintillation light. Emission >540nm = LSO emissionnot absorbed by CdSe
Right: Streak focussed on LSO
This opens the way to composite scintillators, and more generally to metamaterials

## Slide 26: Limits of bulk materials
Performance Limitation
Courtesy of G. Bizzari, Cranfield University

## Slide 27: Towards heterostructures
Performance Optimisation
Courtesy of G. Bizzari, Cranfield University

## Slide 28: Metamaterials
Light transport to SiPM
Photonic crystals, photonic fibers
Prompt emission
Quantum confined (bi)-excitons
in nanocrystals
High stoping power
L(Y,G)SO, (La,Ce)Br3,
BGO, CsI
From the Greek meta-, « metamaterials » means « beyond materials » (i.e. natural materials)

## Slide 29: Metapixels under study
Evaluation of the photodetection efficiency in a sampling geometry with 2 active materials
Evaluation of the energy leakage from the dense to the fast material
CTR estimation from a full MC simulation of prompt and scintillation photons
Notes: CdSe 3% in weight in polystyrène

## Slide 30
LSO
trise = 70ps
Fit on
Rise & decay
Time w/o peak
CdSe/LYSO plates Metapixel
200mm thick LYSO plates
+ 20mm effective thickness
CdSe/CdS nanoplatelet film
3x3x3mm3
S. Gundacker, R. Martinez-Turtos, CERN
Notes: LSO with 70ps rise time

## Slide 31
200mm thick
Naked BGO plates
2x2x3mm3
CdSe/BGO plates Metapixel
200mm thick BGO plates
+ 20mm thick
CdSe/CdS nanoplatelet film
2x2x3mm3
S. Gundacker, R. Martinez-Turtos, CERN

## Slide 32: Energy sharing studies
CTR with
57ps LSO
pixel
BGO block 2x2x3mm3
NUV-HD SiPM 40mm SPAD (FBK)
121ps
BGO DTR=107ps
LYSO DTR=54ps
LYSO block 2x2x3mm3
NUV-HD SiPM 40mm SPAD (FBK)
BC422 DTR=25ps
BC418&BC422 block 2x2x3mm3
NUV-HD SiPM 40mm SPAD (FBK)

## Slide 33
BC422/BGO plates Metapixel
125keV
300keV
200mm thick BGO plates
+ 200mm tBC422
2x2x3mm3
⚫️
110ps
CTR with
57ps LSO
pixel
87ps
CTR with
57ps LSO
pixel
70ps
CTR with
57ps LSO
pixel
87ps
CTR with
57ps LSO
pixel
S. Gundacker, R. Martinez-Turtos, CERN
Notes: BC 422
Light output = LYSO/3
Td —> 1.3ns
Tr —> 30ps CTR nino ~ 50ps

## Slide 34: Considerations for heterostructures design
Keep the density/photofraction close to the scintillator host (BGO, LSO)
Reach a reasonable balance between the standard/prompt photon light yield
Transport efficiently the light from both components
So far, simple and non optimised proof-of-concept designs
BGO comb
UCLA
CdZnS/CdS
CERN
3D printing
200mm ZrO2 plates
100mm holes, 300mm spacing

## Slide 35: Particularities of energy sharing in heterostructures
Timing resolution is different for all events
For a given fraction F of events sharing their energy, the number of events benefiting from a CTR improvement is: F(2-F) > F
  2/3 events share energy in 100mmBGO/100mmBC422
  89% events will have a CTR better than bulk BGO
CTR is much less dependant on detection threshold

## Slide 36: Conclusion- Potential of metamaterials
By making use of light-management strategies, Nanophotonics privides a playground to make the unimaginable come closer.
This opens the way to transformation optics (a kind of extrapolation of Maxwell’s equations invariance under Lorenz transformation), allowing to envision a distortion of real space that results in a desired functionality:
  Ultrafast emission
  Enhanced fluorescence yield through plasmonic resonances
  Redirect light into preferred directions
  Electromagnetic cloaks
  Improve thermal dissipation
  In our case, this is a fertile field for developing innovative solutions for ultrafast
    Light production
    Light transport
    Light photoconversion
Notes: The ability of deep subwavelength plasmonic structures to show strong light–matter interactions is forming the basis of an entirely new class of optical materials.

## Slide 37: The best metapixel requires the best SiPM

## Slide 38: New SiPM concept
The Quantum Silicon Detector

## Slide 39
The 10ps challenge:
  a spur on the development of fast timing
  an opportunity to get together
  an incentive to raise funding
  a way to shed light on nuclear instrumentation for medical imaging
One unique challenge launched for 5 to 10 years and operated by an international organisation with rules issued by the community based on the measurement of CTR combined to sensitivity
Several milestones and prices:
  3 years after the launch of the challenge: 1M€ expected for the Flash Gordon prices for the realisation of 3 important milestones
  until the end of the challenge: 1M€ expected for the Leonard McCoy price for the first team meeting successfully the specifications of the challenge
Notes: The essence of a challenge is to think big and to gather the multidisciplinarity expertise for a real breakthrough
We have of course to assume the risk of an ambitious challenge
In my view the most important risk is to underestimate the physical barriers (ex. The Heisenberg uncertainty principle )
The two other risks that need to be considered are:
  The technological risk:
    can we find a technology or a combination of technologies that will provide a solution to the challenge
    Answer: if there are no physical barrier, solutions will be developed, sooner or later
  The cost:
    Can be mitigated by the progress of the technologies and the importance of the impact

## Slide 40: Conclusion
“Impossible”
is not a French word
Napoléon
Disruptive technologies
Nano-photonics
New, intelligent
Multifunctional sensors
New
perspectives
Notes: A number of disruptive technologies, particularly in the very rich domain of nano-photonics open completely new perspectives for new, intelligent and multifunctional sensors

## Slide 41: Many thanks to
Notes: At this stage I need to thank many people, first of all my group at CERN, which is now run very efficiently by Etiennette Auffray
But also a number of colleagues, all over the world, for their encouragements and stimulating and enriching discussions
CERN and the European commisssion for the financial support through a number of projects, all related to fast timing
And I would not like to forget all of you for your attention

## Slide 42: Meta-X-g Detector Block for Low Energy Applications
Heavy scintillating fibers
(LuAG, LSO …)
F = 500mm
Quantum dot
loaded polymer
with a gradient
of QD radius
along the fibre
Photonic fibers
F = 100mm
Shown at NSS/MIC 2008, Dresden